## Slide 1: A density functional theory of nematic liquid crystals with long-range attractive & short-range repulsive interactions
Peter Palffy-Muhoray Liquid Crystal Institute, KSU
Mikhailo Pevnyi Liquid Crystal Institute, KSU
Epifanio Virga Dept. of Mathematics, U. Pavia
Xiaoyu Zheng Dept. of Math. Sciences, KSU
Notes: Autonomous: having self-directing freedom

## Slide 2: Outline
motivation
background
model
phase separation
Landau expansion
summary

## Slide 3
Motivation

## Slide 4: Motivation
liquid crystal phase is interesting and important
in spite of considerable study, still incompletely understood
phenomena of particular interest:
  dependence of density and orientational order on temperature and pressure

## Slide 5: Motivation
P.P-M., D.A. Balzarini, Can. J. Phys., 59, 1981
temperature dependence of density
Notes: Both steric and attractive interactions play a role.

## Slide 6: Motivation
liquid crystal phase is interesting and important
in spite of considerable study, still incompletely understood
phenomena of interest:
  dependence of density and orientational order on temperature and pressure
  phase coexistence in pure materials

## Slide 7: Motivation
coexisting nematic and isotropic phases
O.D. Lavrentovich, priv. comm.
Notes: Phase rule; P=C - F+2 (F = free intensive variables)

## Slide 8: Motivation
liquid crystal phase is interesting and important
in spite of considerable study, still incompletely understood
phenomena of interest:
  dependence of density and orientational order on temperature and pressure
  phase coexistence in pure materials
need complete equation of state to describe phenomena

## Slide 9
Background

## Slide 10: Background
LCs:
  (usually ) liquids
  characterized by orientational order
  large variety of phases:
  +….etc.

## Slide 11: Orientation in Nematic Liquid Crystals
orientation descriptor:
  second rank tensor
orientational order parameter:
  traceless symmetric

## Slide 12: Nematic liquid crystals
order parameter:
  symmetric traceless tensor
eigenvectors:
  direction of alignment:
  nematic director
eigenvalues:
  degree of alignment:
  order parameter

## Slide 13: Background
nematic LCs:
  thermotropic:
    orientational order & related properties depend on temperature
  lyotropic:
    orientational order & related properties depend on concentration

## Slide 14: Models for nematics
thermotropics:
  Maier-Saupe1
  Frank, Landau – de Gennes
    attractive long-range interactions
    temperature dependent description; density assumed constant
lyotropics:
  Onsager2
    repulsive short-range hard-core interactions
    concentration dependent description; athermal
W. Maier and A. Saupe A., Z. Naturforsch. A 14, 882., (1959).
L. Onsager, Ann. NY Acad. Sci. 51, 627 (1949).

## Slide 15: Background
nematic LCs:
  thermotropic:
    orientational order & related properties depend on temperature
  lyotropic:
    orientational order & related properties depend on concentration
but lyotropics respond to temperature,
and thermotropics respond to pressure!

## Slide 16: Aim
develop simple model
  incorporating both attractive & steric interactions
  capable of describing multicomponent systems
study predictions & compare with experiment
what is needed in model?
  free energy of multicomponent system in density functional form, including hard and soft interactions

## Slide 17
Model

## Slide 18: Free energy
Helmholtz free energy
partition function:
    generalized coordinate & momenta
configurational partition function:
  (integrate out momenta)
pairwise interactions:

## Slide 19: Free energy
have
one can show
what is the pair potential ?

## Slide 20: Pair potential
two parts:
attractive London dispersion
  quantum fluctuation creates ‘spontaneous’ dipole in one particle
  the field of this dipole polarizes the second; two dipoles attract
‘hard core’ repulsion
  Pauli exclusion principle forbids overlap of electron orbits
  ‘hard’, overlap energy comparable to ionization

## Slide 21: London dispersion
for two spheres,
for ellipsoids,
where
R
Notes: hv ~ 200kT, if R=2r, U~kT. Things melt, etc. Magic!

## Slide 22: London dispersion
for ellipsoids,
or
Notes: hv ~ 200kT, if R=2r, U~kT. Things melt, etc. Magic!

## Slide 23: Hard core repulsion
treat particles as rigid bodies
relevant quantity: excluded volume

## Slide 24: Excluded volume
Onsager1 :
  long cylinders
this work (2)
  ellipsoids
cylinders
ellipsoids
1. L. Onsager, Ann. NY Acad. Sci. 51, 627 (1949).
2. Priestley, Wojtowicz and Sheng, Introduction to liquid crystals. (Plenum , NY 1975)

## Slide 25: Free energy
have
for the attractive part, assume
MF energy

## Slide 26: Free energy
have
for repulsive part, assume
MF volume

## Slide 27: Helmholtz free energy
free energy
becomes
density functional form?

## Slide 28: Density functional form
if density is not uniform, we can write locally in region
and summing over all regions of phase space,

## Slide 29: Density functional form
and have
where
ideal gas
long range attractive
short range repulsive

## Slide 30: Low density regime
expanding the logarithm, have
where
ideal gas
Maier-Saupe
~Onsager

## Slide 31: Helmholtz Free Energy (expanded log term)
letting and
substituting for and gives

## Slide 32: The Orientational Distribution
minimizing wrt gives
where is the volume fraction,
and is the anisotropic interaction strength

## Slide 33: Free energy
with this the free energy density becomes
where and
and minimizing wrt gives the self-consistent equation

## Slide 34: Modified Onsager theory (a=b=0)
Lyotropic Ordering
Isotropic
Nematic
first order
unstable
metastable
stable
nematic
Isotropic
Order parameter S vs.

## Slide 35: Maier-Saupe theory (c=d=0)
Thermotropic Ordering
Isotropic
Nematic
first order
order parameter S vs T
Isotropic
unstable
metastable
stable
nematic

## Slide 36: M-S--O Results
Order parameter vs. temp and number density
Notes: MS: rho=0, O: T=inf

## Slide 37: M-S--O Results
Order parameter vs. temp and number density
Free energy for different solutions

## Slide 38: Equation of State
change variables:
  single control parameter:

## Slide 39: Equation of State
pressure is given by
and substitution gives
in qualitative agreement with experiment

## Slide 40: Equation of State
pressure is given by
and substitution gives
in qualitative agreement with experiment
Problem: density remains finite regardless of !

## Slide 41: Phase separation in a one component nematic

## Slide 42: Phase separation
single component
for coexistence, must have, in each phase, equal
  chemical potential
  pressure
equivalent to double tangent construction on .

## Slide 43: Another look at the free energy
change variables:
  single control parameter:

## Slide 44: Double tangent construction
plot vs.
  in general, have three branches: , ,
  two
construct
double tangents
challenging!

## Slide 45: Another approach:
plot pressure vs. chemical potential
with as parameter
at coexistence, curve should cross over itself

## Slide 46: Pressure vs chemical potential
nematic S+
nematic S-
isotropic S=0

## Slide 47: Pressure vs chemical potential
slope becomes
discontinuous

## Slide 48: Pressure vs chemical potential
??

## Slide 49: Pressure vs chemical potential
curve folds back
& crosses itself
nematic – nematic
coexistence?

## Slide 50: Pressure vs chemical potential
nematic – isotropic
coexistence

## Slide 51: Pressure vs chemical potential
Swallowtail Catastrophe

## Slide 52: In 3D

## Slide 53: Pressure vs chemical potential
3 crossings:
N-N,
N-I1,
N-I2
3 pairs of coexisting phases??

## Slide 54: The three instances of equal and equal

## Slide 55: Corresponding double tangent constructions

## Slide 56: Double tangent constructions
multiple double tangent constructions are possible
(even ignoring S- branch)
only one - nematic-isotropic coexistence - minimizes the free energy

## Slide 57: Phase diagram
nematic
nematic
isotropic
2-phase
coexistence
0.781
isotropic

## Slide 58: Phase diagram
N
N
I
I
0.781
Notes: No

## Slide 59: Landau Free Energy
can behavior be captured in simpler model?
Landau free energy
  expansion in terms of order parameter

## Slide 60: Landau expansion
free energy in Landau form
  where and
have two options:
  keep full dependence
  replace dependent coefficients by constants.

## Slide 61: Two phase coexistence
using
carry out double tangent construction

## Slide 62: Two phase coexistence
and arrive at phase diagram

## Slide 63: Summary
derived density functional form of free energy with attractive and repulsive contributions
steric contributions appear in logarithm
low density approximation, gives simple expression for free energy combining M-S and Onsager
single control parameter
interesting NI coexistence prediction
Landau theory description also possible

## Slide 64: Acknowledgements
Mikhailo Pevnyi
Epifanio Virga
Xiaou Zheng