## Slide 1: The effect of nonlocality on material stability
Stewart Silling
July 18, 2022
Theoretical and Applied Aspects for Nonlocal Models
Banff International Research Station
SAND2022-9623 C

## Slide 2: Outline
The nonlocal length scale affects all aspects of material stability.
  Failure kinetics: “Imaginary wave speeds” are useful.
  Material and structural instability are related, leading to models for:
      Kink bands in composites.
      Self-shaping of fibers.
  Phase boundaries contain an unstable core.
    Their motion lowers the energy in a polycrystal by reshaping and merging grains.

## Slide 3: Some concepts of stability (local theory)
Real wave speeds (Hadamard stability, strong ellipticity)
Minimum potential energy
Bifurcations
Well-posedness*
Discontinuity in gradient (Ordinary ellipticity)
*Summary of well-posedness result for nonlocal theories: see:
Qiang Du, "Nonlocal calculus of variations and well-posedness of peridynamics." Handbook of peridynamic modeling. (2016)
R. Lipton’s papers on nonconvex strain energy in crack nucleation.

## Slide 4: Material vs. structural stability (local theory)
Material instability:
  Happens at a material point, triggered by local conditions
  Not directly related to the geometry of the body
  Example: Adiabatic shear band
Structural instability:
  Happens to the entire body collectively
  Example: Buckling of a beam
Adiabatic shear band in aluminum
image: Baxevanis et al.,
www.ima.umn.edu/materials/2008-2009/SP7.13-31.09/8186/ima.pdf
Buckling of a column
image: Klimchik
www.researchgate.net/figure/Examples-of-buckling-in-column-www-civildb-www-highline_fig11_281183936
We’ll see that this distinction becomes less useful in a nonlocal model.

## Slide 5: Peridynamics background
Bond
Time
Time

## Slide 6: Linear bond force model

## Slide 7: An intuitive notion of stability… and a mysterious tensor
Comparable statement in the local theory:

## Slide 8: Simplify further to 1D, linear microelastic
Some possible micromodulus curves

## Slide 9: Linear waves: Dispersion curves
Some possible dispersion curves
We’ve seen this before!

## Slide 10: Dispersion and material stability
Micromodulus curves
Dispersion curves
Stable
Unstable
Purple and red materials have “imaginary wave speeds” .
  Red: all wavenumbers are unstable.
  Purple: only some wavenumbers are unstable.
is not required for real wave speeds*
*T. Mengesha, and Q. Du., Discrete & Continuous Dynamical Systems-B (2013).

## Slide 11: Example: A material with a narrow band of unstable wavenumbers
0
1.0
0.5
1.5
Bond length
Micromodulus
0
Material model
0
20
10
Wave number
Frequency squared
0
Wavelength = 0.5
Dispersion curve
Stable
Unstable
Unstable wavelength

## Slide 12: This material is stable in some geometries but unstable in others
Short bar (length = 1.0)
Long bar (length = 2.0)
Unstable wavelength
Unstable wavelength
VIDEOS

## Slide 13: Similar problem in the local theory blows up immediately
Strain
Stress
We can’t “do mechanics” in an unstable material in the local theory.

## Slide 14: Failure kinetics: Unstable waveforms grow exponentially but at a finite rate

## Slide 15: How much time does it take for an unstable waveform to grow?
0
1
2
0
0.1
0.2
Strain
Time
Growth of a perturbation for different wavelengths
Bond force
Bond strain
Peridynamic material model
Suppose the material “fails” when the local strain exceeds some given value .

## Slide 16: Failure kinetics: How much time does it take for material to fail?
Example: Stretching of a bar with an unstable material model.
  Bar is stretched from the ends at a constant rate.
  The bond force vs. strain curve has a descending branch.
  What happens?
Weak spot
Strain rate
Bond strain
Bond force
Material model
Stress at center
Strain at center
Time
Numerical simulation results
Failure time

## Slide 17: Self-shaping of a fiber
String made of microelastic material
Constant long-range forces between material points
Allow rotations (unlike true 1D)
Study transverse waves and their stability
Wave velocity
Fiber
Internal force
Area
Fiber

## Slide 18: Internal loading in a fiber accounting for bond rotations
Internal loading as a function of bond length

## Slide 19: Transverse waves
Stable
Unstable

## Slide 20: If a straight fiber is unstable, what does equilibrium look like?
Slope =
We can compute* the curvature of a fiber in equilibrium.
Result:
Straight is unstable
Curvature
Straight is stable
* SS, “Self-induced curvature in an internally loading peridynamic fiber,” technical report SAND2022-5539

## Slide 21: Emu simulation of an internally loaded fiber
Initial
Final
VIDEO
Colors show strain
(red = 0.01)
Internal loading is turned on suddenly.

## Slide 22: Homogenized model of many fibers: Kink bands in a fiber-reinforced composite
Transverse wave
Fibers in a matrix
Remote loading in fibers is
Bonds can be either stiff or soft

## Slide 23: Emu simulation of instability in compression in a composite
Kink band in a composite
Image: S.P.H. Skovsgard, thesis, 2019
Initial
Final
Colors show displacement magnitude
Bonds in the horizontal direction are more stiff than the others.
Anisotropic, microelastic material model.
There is no damage (bond breakage) in the peridynamic model.
Time
Load in x-direction
Compressive failure

## Slide 24: Mechanically induced phase transformation
Here’s another type of nonconvex microelastic material:
Bond strain
Bond force
Low strain phase
High strain phase
Phase boundary (thickness )
There are multiple bond strains for the same bond force.
This creates the possibility of multiple phases in a bar in equilibrium.
Within the phase boundary, there are always some bonds in the unstable part of the material model.
K. Dayal & K. Bhattacharya. J. Mechanics & Physics of Solids (2006).

## Slide 25: What conditions permit coexistent phases?
In equilibrium, energy conservation implies
which is formally the same as in the local theory.
Compare Weierstrass corner condition, Maxwell condition in the calculus of variations.
Phase boundary (thickness )

## Slide 26: Microstructure evolution
The system evolves over time to reduce the total surface area of phase boundaries.
We can use this to simulate microstructure evolution.
Bond strain
Bond force
density
Both these grains if isolated have zero stress, energy
Strain =
Strain = 0
But it they share an edge, they distort and their energy increases.

## Slide 27: Circular grain evolution
VIDEOS
Colors show bond strain
Initialize a displacement field to have zero strain inside a circle, outside.
Either all purple or all yellow would be a global minimizer
Bond strain
Bond force
density

## Slide 28: Microstructure evolution over time
VIDEO
Colors show bond strain
Voronoi cells (grains) have random initial strain.
Mismatch of strains at grain boundaries causes strain energy.
Total energy is reduced by merging small grains to form larger grains.

## Slide 29: Summary
Nonlocality changes everything about material stability.
We can do meaningful continuum mechanics within an unstable material.
We can use this to simulate real phenomena:
  Rate of crack nucleation in response to a suddenly applied load
  Self shaping of a long molecule
  Compressive failure modes in composites
  Microstructure evolution
Special thanks to our IT specialist

## Slide 30: Extra slides

## Slide 31: Minimum potential energy is related to wave speed

## Slide 32: Minimum potential energy is related to wave speed, ctd.

## Slide 33: Minimum energy implies real wave speeds

## Slide 34: Stretching of a bar: Compute the time to failure
Bond force
Bond strain
0.001
0.01
0.1
1
10
Strain rate
100
10
1
0.1
0.01
Failure time
Failure time
Weak spot
Strain rate

## Slide 35: Stretching of a bar: We arrive at a macroscopic rate effect
It takes time for the bar to fail even after some bonds have crossed the peak.
Meanwhile, the remote strain is still increasing.
Result is that higher strain rates lead to higher macroscopic failure strain
Many real materials show a similar trend.
Remote strain at time of failure
Strength
Rate effect on the strength of polyethylene
(Yu, Lu, & Cai, 2013)
SS, Journal of Peridynamics & Nonlocal Modeling (2021)

## Slide 36: Crack nucleation as a material instability
A body is initially continuous.
At some later time there is a discontinuity.
What mathematical conditions need to exist for this to happen?
  This question is not addressed by fracture mechanics, which assumes a pre-existing defect.
SS, O. Weckner, E. Askari & F. Bobaru, Int. J. Fracture (2010)
R.P. Lipton, R.B. Lehoucq & P.K. Jha, J. Peridynamics & Nonlocal Modeling (2019)

## Slide 37: Perturbation by a jump
Suppose a small virtual discontinuity is inserted into a body under load.
Does the discontinuity grow or close up?
Analyze the evolution of the jump .

## Slide 38: Perturbation by a jump

## Slide 39: A nonlocal model of fracture can be well-posed (!)
Nonconvex elastic peridynamic material.
Points entering the unstable branch lead to creation of a jump in displacement.
This discontinuity can grow through the body.
As it grows, it consumes a definite amount of potential energy per unit crack area (Griffith crack).
The whole problem can be well-posed.
These results hold for both static and dynamic cases.
Bond strain
Bond force
R.P. Lipton, J. Elasticity (2014)
R.P. Lipton, J. Elasticity (2016)
P.K. Jha & R.P. Lipton, SIAM J. Numerical Analysis (2018)
R. Lipton, E. Said & P.K. Jha - Handbook of nonlocal continuum mechanics for materials and structures (2018)
R.P. Lipton, R.B. Lehoucq & P.K. Jha, J. Peridynamics & Nonlocal Modeling (2019)
P.K. Jha & R.P. Lipton, Computer Methods in Applied Mechanics & Engineering (2019)
R.P. Lipton & P.K. Jha, Nonlinear Differential Equations and Applications (2021)

## Slide 40: at the crack nucleation site and near a growing crack tip
Material model
There is a process zone near a growing crack tip within which